Processing of silicon detectors

| Day | Processing | Measurement | Notes |
| --- | --- | --- | --- |
| 1 | Starting wafer |  |  |
| 1 | Standard Cleaning |  |  |
| 1 | Oxide growth, wet 1050۫ C, 1 hour, doping n+ backside and growth of silicon-dioxide |  |  |
| 2 | Unload wafers | Oxide thickness |  |
| 2 | Spinning of resist, 4000 rpm, 1.8 um positive resist, front and backside |  |  |
| 2 | Softbake, 92 ۫ C, 1 min hotplate, 15 min furnace |  |  |
| 2 | Patterning mask 1 |  |  |
| 2 | Development 1 min/ rinsing |  |  |
| 2 | Inspection |  |  |
| 2 | Hardbake 120 C, 15 min |  |  |
| 2 | Etching with buffered HF until hydrofobic openings/ rinsing |  |  |
| 2 | Stripping of resist |  |  |
| 2 | Standard cleaning |  |  |
| 2 | Loading doping furnace,950 C 1 hour |  |  |
| 3 | Unload furnace | Measure monitor wafer |  |
| 3 | Opening of p-areas, 5% HF/ rinsing |  |  |
| 3 | Evaporation of Aluminium, 3000Å |  |  |
| 3 | Patterning mask 2 |  |  |
| 3 | Development 1 min/rinsing |  |  |
| 3 | Inspection |  |  |
| 3 | Hardbake 120 C, 1 min |  |  |
| 3 | Etching of Aluminium/ rinsing |  |  |
| 3 | Spinning of resist front side |  |  |
| 3 | Etching backside hydrophobic/ rinsing |  |  |
| 3 | Evaporation of Aluminium, 3000Å |  |  |
| 3 | Stripping of resist |  |  |
| 3 | Cold sulphuric acid 1 min/ rinse |  |  |
| 3 | Forming gas annealing |  |  |
| 4 | Probe station, measurement |  |  |