Processing of silicon detectors_ver b

| Day | Processing | Measurement | Notes |
| --- | --- | --- | --- |
| 1 | Starting wafer |  |  |
| 1 | Standard Cleaning |  |  |
| 1 | Oxide growth, wet 1050۫ C, 1 hour, doping n+ backside and growth of silicon-dioxide |  |  |
| 2 | Unload Wafer | Oxide thickness |  |
| 2 | Mark “B” on backside Spinning of resist, 4000 rpm 1.8 um positive resist, frontside |  |  |
| 2 | Hardbake 120 C, 1 min hotplate |  |  |
| 2 | Etching with buffered HF until Backside hydrophobic (~8 min)/ rinsing 4 min/ spin and dry “oxide” |  |  |
| 2 | Stripping of resist, 1165, 5 min/ rinse 5 min/ spin and dry |  |  |
| 2 | Standard cleaning, ”7-up” for 10 min, 3 min bubbler, 3 min Imec, 3 min bubbler, rinse and spin |  |  |
| 2 | Load Phosphorus furnace 900C/ 30 min |  |  |
| 3 | Unload wafer |  |  |
| 3 | Etch backside hydrophobic 1:10 HF/ 1min, rinse 3 min, rinse and spin |  |  |
| 3 | Oxide growth, wet 1050۫ C, 1 hour, doping n+ backside and growth of silicon-dioxide |  |  |
| 4 | Unload wafers |  |  |
| 4 | Spinning of resist, 4000 rpm, 1.8 um positive resist, front and backside |  |  |
| 4 | Softbake, 115 ۫ C, 1 min hotplate, 15 min furnace |  |  |
| 4 | Patterning mask 1 |  |  |
| 4 | Development 1 min/ rinsing |  |  |
| 4 | Inspection |  |  |
| 4 | Hardbake 120 C, 15 min |  |  |
| 4 | Etching with buffered HF until hydrofobic openings/ rinsing |  |  |
| 4 | Stripping of resist |  |  |
| 4 | Standard cleaning |  |  |
| 4 | Loading doping furnace,950 C 1 hour |  |  |
| 5 | Unload furnace | Measure monitor wafer |  |
| 5 | Opening of p-areas, 5% HF/ rinsing |  |  |
| 5 | Evaporation of Aluminium, 3000Å |  |  |
| 5 | Patterning mask 2 |  |  |
| 5 | Development 1 min/rinsing |  |  |
| 5 | Inspection |  |  |
| 5 | Hardbake 120 C, 1 min |  |  |
| 5 | Etching of Aluminium/ rinsing |  |  |
| 5 | Spinning of resist front side |  |  |
| 5 | Etching backside hydrophobic/ rinsing |  |  |
| 5 | Evaporation of Aluminium, 3000Å |  |  |
| 5 | Stripping of resist |  |  |
| 5 | Cold sulphuric acid 1 min/ rinse |  |  |
| 5 | Forming gas annealing |  |  |
| 6 | Probe station, measurement |  |  |